HMD(S)06-LC 防眩光PC优点防眩光、AF防指纹、抗冲击、韧性好, 可应用于对硬度要求较低的需要防反射的产品，如功能机镜片、小家电面板、防护眼镜、安防面板和电梯户外广告牌等PC anti glare board has the advantages of anti glare, AF anti fingerprint, anti impact and good toughness. It is mainly used in products with low hardness requirements, such as functional lens, small household appliance panel, protective glasses, security panel and elevator outdoor billboard.

HMD(S)06-LA 防眩光PMMA优点防眩光、AF防指纹、硬度高、钢性强，可应用于对表面硬度要求较高的需要防反射产品，如空调面板、医疗器械面板、智能家居面板和汽车充电桩面板等PMMA anti glare board has the advantages of anti glare, AF anti fingerprint, high hardness and strong rigidity. It is mainly used in products with high surface hardness requirements, such as air conditioning panel, medical device panel, smart home panel and automobile charging pile panel.

HMD(S)06-2L 防眩光板复合板优点防眩光、AF防指纹、硬度高且抗冲击性能强，可应用于对硬度抗冲击均有要求的需要防反射产品，例如手机电池盖、电子书触摸镜片及电池盖等 two-layer composite board anti glare board has the advantages of anti glare, AF anti fingerprint, high hardness and strong impact resistance. It is mainly used in products with requirements for hardness and impact resistance, such as mobile phone battery cover, e-book touch lens and battery cover.

HMD(S)06-3L 防眩光三层复合板优点防眩光、AF防指纹、低翘曲、钢性强，可应用于一些高端要求的需要防反射产品，例如车载仪表盘和中控面板等 Three layer composite board anti glare board has the advantages of low warpage, good flatness, anti glare, AF anti fingerprint and strong rigidity. It is mainly used in some high-end products, such as vehicle dashboard and central control panell.

| 材料型号 Plate type | 颜色 Color | 特征 Feature | 厚度（mm） Thickness | 有效尺寸（mm) Effective size |
| --- | --- | --- | --- | --- |
| HMD(S)06-LC AG防眩光PC | 雾面/磨砂 Fog / Frosting | 防刮花 /防眩光 /AF防指纹 Anti scratch/ Anti-Glare/AF | 0.175mm-4.0mm | 1120mm*1710mm |
| HMD(S)06-LA AG防眩光PMMA | 雾面/磨砂 Fog / Frosting | 防刮花 /防眩光 /AF防指纹 Anti scratch/ Anti-Glare/AF | 0.5mm-4.0mm | 1130mm*1560mm 1130mm*1710mm |
| HMD(S)06-2L AG防眩光复合板 | 雾面/磨砂 Fog / Frosting | 防刮花 /防眩光 /AF防指纹 Anti scratch/ Anti-Glare/AF | 0.25mm-2.0mm | 1130mm*1880mm |
| HMD(S)06-3L AG防眩光三层复合板 | 雾面/磨砂 Fog / Frosting | 防刮花 /防眩光 /AF防指纹 Anti scratch/ Anti-Glare/AF | 0.65mm-2.0mm | 1130mm*1880mm |

板材结构图

- PC、PMMA、PC+PMMA

- PMMA+PC+PMMA

保护膜Protective film

AG防眩光涂层Anti-Glare coating layer

防刮花涂层Hard coating layer

颜色保护膜Protective film

基材Substrate

Structure diagram

Typical Property Values

| AG防眩光板材 AG Anti-Glare sheet |  |  |  |  |  | 测试方法 Test method |
| --- | --- | --- | --- | --- | --- | --- |
| 型号 Model | HMD(S)06-LC |  | HMD(S)06-LA | HMD(S)06-2L | HMD(S)06-3L | / |
| 基材 Substrate | PC材质 | PMMA材质 |  | PC+PMMA材质 | PMMA+PC+PMMA材质 | / |
| 厚度 Thickness | 0.175-4.0mm ±0.05 | 0.4-4.0mm ±0.05 |  | 0.25-2.0mm ±0.05 | 0.65-2.0mm ±0.05 | 千分尺 Micrometer |
| 透光率 Transmittance | ≥90% | ≥90% |  | ≥90% | ≥90% | ASTMD1003 |
| 雾度 Haze | 8±2% （雾度可定制1-80%） | 8±2% （雾度可定制1-80%） |  | 8±2% （雾度可定制1-80%） | 8±2% （雾度可定制1-80%） | ISO14732 |
| 光泽度60° Gloss 60° | 95±15 | 95±15 |  | 95±15 | 95±15 | 光泽仪 Glossmeter |
| 粗糙度（Ra) Roughness(Ra) | 0.06-0.09 | 0.06-0.09 |  | 0.06-0.09 | 0.06-0.09 | 粗糙度测试仪 Roughness tester |
| 表面硬度 Pencil hardness | HB | 4H |  | PC:HB PMMA：4H 0.5mm厚度以下PMMA面：2-3H | 4H | PC：500g,PMMA:750g 法码，三菱铅笔划痕 PC:500g,PMMA:750g Farmar, MITSUBISHI pencil scratch |
| 耐磨性 Abrasion resistance | 外观无变化 No change in appearance | 外观无变化 No change in appearance |  | 外观无变化 No change in appearance | 外观无变化 No change in appearance | 绑无尘布，20mm*20mm，负重1kg，磨擦2000次 Tied dust-free cloth, 20mm*20mm, weight 1kg, friction 2000 times |
| 水滴角 Water Drop angle | ≥105° | ≥105° |  | ≥105° | ≥105° | 水滴角测量仪 Water drop angle measuring instrument |
| 燃烧性UL94 Combustibility | HB-V2 | HB |  | HB-V2 | HB-V2 | UL94 |
| 收缩率 Shrinkage rate | 0.2% | 0.3% |  | 0.2% | 0.2% | ASTM D1204 |
| 膜层附着性 Film adhesion | 5B | 5B |  | 5B | 5B | ASTM D3359 |

这些都是典型的属性,不用于规范的目的。如果最低可确认的属性是必需的,请联系我公司的业务为您服务。

These are typical properties and are not intended for specification purposes. If minimum certifiable properties are required, please contact my company's business to serve you.